## Slide 1
Megan Jackson, Onyu Jung
Surendranath Group, MIT
ONR In-person Meeting
Feb 22, 2018
Molecular control of interfacial proton-coupled electron transfer
Notes: Introduce
5 months

## Slide 2: HER on Au proceeds through rate-limiting CPET
Rate of HER on Au is rate of CPET
Rate-limiting electron transfer
First order in H3O+
Norskov, J; et al. J. Electrochem. Soc. 2005, 152, J23.
Notes: point to low adsorption energy of H on Au (computation Norskov JES – schmickler).
J is related to rate (have on slide and state)
Show data w/o slope and say j is related to rate
Why is it log/linear? Arrhenius eqn=> changing delta G double dagger gives change in rate
Have slopes appear and say it’s informative
Then equations
Either don’t use marcus curves or label products and reactants on the wells

## Slide 3: pH-dependence of HER in aqueous media
H3O+ donor?
H2O donor?
Inverse order in pH?
No pH-dependence?
pH scale

## Slide 4: Choice of electrolyte
Borate (pKa = 9.1)
Formate (pKa = 3.75)
~ 0.1
Formate and borate buffers do not seem to contribute of the kinetics of HER.
They allow direct measurement of pH-dependence of HER across the pH range

## Slide 5: pH-dependent Tafel slope
~120 mV dec-1
60-90 mV dec-1
The Tafel slope of HER is 60 to 90 mV/dec at very low pH, and increases to 120 mV/dec at intermediate to high pH.

## Slide 6: HER is first-order at low pH and half-order at high pH
Low pH
High pH
Order in [H+]:

## Slide 7: What is the origin of the half order?
Is the PZC changing with pH?
Fractional order suggests adsorption. Is there pH-dependent surface adsorption at intermediate and high pH?
or
?
~120 mV dec-1
60-90 mV dec-1

## Slide 8: No diffusion or migration effects observed
Similar activity observed at different rotation rates
Similar activity observed with different concentrations of supporting electrolyte